## Slide 1: Polymer Enclosure with Wire Passthrough for Implantable Device
Neuralink, US 2023/0148968 A1, Published 5/18/2023
6/17/2024

## Slide 2: Background
Implantable devices in-vivo have rigid hermetic housing to protect active electronics from environmental and mechanical stress
Increasingly common for large number (e.g., thousands) of tightly-spaced (micron-level spaced) wires extending from implantable device
Traditional housing materials (ceramic, glass, titanium) can become problematic with above structure (e.g., cracked glass housing)

## Slide 3: Outline
Goal: Describe a method and disclosure for manufacturing polymer (PCTFE) enclosure with polymer (PI) wires extending through a passthrough slit for implantable devices + reflowing process to form substantially hermetic seal around wires
Purpose of invention: To prevent bending or straining of wires and allow the use in relatively high temperatures and pressure to ensure substantially hermetic seal.
Embodiments:
  Implantable Device with Polymer Enclosure with Bottom Passthrough Slit
  Components of Enclosure
  Piece of Polymer Before and During Slit Fabrication
  Piece of Polymer with Insulated Wires Inserted in Slit
  Portion of Enclosure Placed in Mold for Sealing
  Piece of Polymer Placed in Mold Base for Sealing
  Clamp for Sealing Passthrough Slit
  Heater for Sealing Passthrough Slit
  First View of Mold for Manufacturing a Polymer Enclosure
  Second View of Mold for Manufacturing a Polymer Enclosure, with Wires in Place
  Mold for Manufacturing a Polymer Enclosure, with Wires and Stiffener in Place
  Flowchart for Manufacturing Enclosure with Passthrough Slit
  Computer System

## Slide 4: Implantable Device with Polymer Enclosure with Bottom Passthrough Slit
Enclosure
First piece of polymer (bottom portion; PCTFE)
Second piece of polymer (top portion; PCTFE)
Slit
Insulated wires
In the form of polymide (PI) electrode film array
Parallel to each other
Perpendicular to first PCTFE portion
Spaced by < 100 micrometers
Each wire - includes metal traces (not visible), spaced by 2, 2 cross-sectional width
Metal trace – one end with device, one end with electrode
Attachment means
Edge
* Inside the structure (sealed): IC chip, communications components (wireless, bluetooth), power components (wireless charging)

## Slide 5: Components of Enclosure
First piece of polymer
Second piece of polymer
Insulated wires

## Slide 6: Piece of Polymer in Slit Fabrication Process
Slit
Forceps / tweezers
Piece of polymer (PCTFE)
Before
slit fabrication
(initial piece of PCTFE provided)
During
slit fabrication
(slit formed via knife or blade, cut may be partial or completely separating)
During
slit fabrication
(slit widened via tweezers/forceps to accommodate wires, then sanded/smoothed to prevent damage)

## Slide 7: Piece of Polymer with Insulated Wires Inserted in Slit
Piece of polymer
Slit
Wires (pass through slit, annealed at temperature < 100C)

## Slide 8: Portion of Enclosure Placed in Mold for Sealing
Insulated wires
Slit
Mold Base
(PCTFE fits snugly inside mold base, facilitate reflow of PCTFE to seal around wires)
Piece of polymer (PCTFE)

## Slide 9: Piece of Polymer Placed in Mold Base for Sealing
Insulated wires
Mold Base
Mold Top
Mold
made of metal or other rigid material that does not decompose, deform, or react chemically with polymer at reflow temperature/pressure
Follow outline pattern of PCTFE to fit PCTFE snugly (PCTFE does not move around)
PCTFE (not visible) enclosed within mold

## Slide 10: Clamp for Sealing Passthrough Slit
Clamp:
- Used to apply pressure to portion with slit & insulated wires for thermocompression
- C-clamp shown

## Slide 11: Heater for Sealing Passthrough Slit
Heater:
- Used to apply heat to portion with slit & insulated wires for thermocompression
- Furnace – heat to 200-400C

## Slide 12: First View of Mold for Manufacturing a Polymer Enclosure
Mold Base
(polymer reflows within mold)
Mold Top
Opening
(where wires extend out)

## Slide 13: Second View of Mold for Manufacturing a Polymer Enclosure, with Wires in Place
Mold Top
Opening
Mold Base
Wires
Melt zone
Piece of polymer
Bond pad region
Electrode region
If wires are pre-connected to electronics before slit formation  bond pad OUTSIDE of mold (prevent damage to electronics)

## Slide 14: Mold for Manufacturing a Polymer Enclosure, with Wires and Stiffener in Place
Mold Top
Mold Base
Opening
Wires
Piece of polymer
Melt zone
Stiffener
Placed between polymer & mold
Temporarily support wires during sealing
Protect wires from damage
Maintain alignment of wires
Made of Kapton (polymide film type)

## Slide 15: Flowchart for Manufacturing Enclosure with Passthrough Slit

## Slide 16: Step 1:
Piece of polymer
Insulated wires

## Slide 17: Step 2:
Piece of polymer
Slit
Forceps/Tweezers
Form slit via knife/blade
Widen slit via forceps, then sand down to accommodate wires

## Slide 18: Step 3:
Piece of polymer
Slit
Wires
Mold Top
Mold Base
Opening
Wires
Piece of polymer
Melt zone
Stiffener

## Slide 19: Step 4:
Heater
Clamp
Use thermo-compression techniques for thermal bonding PCTFE (performed automatically in controller)
Seal slit around wires
  Apply pressure on polymer piece + insulated wires on the slit portion via clamp (or hydraulic press/piston)
  Heat polymer + wires via furnace (or hot plate) – melt polymer without damaging wires (250-300C for PCTFE polymer piece for reflow + fusing around PI wires, 10-15 minutes)
    Higher pressure, time, temperature of thermocompression  more PCTFE melt
Deactivate heater & clamping devices from mold
Dispose active electronics within 2 polymer pieces
Join 2 polymer pieces to form enclosure (similar to step 1, but set max temperature to 255-260C)
Cool implantable device (sealing system sets alarm to notify user of completion)
* reflow: join metals together by heating and melting solder

## Slide 20: Computer System