## Slide 1: Die Reconstruction and High-Density Interconnects for Embedded Chips
Neuralink, US 2024/0128222 A1, Published 4/18/2024
6/17/2024

## Slide 2: Background
Implantable devices can be implanted into neurological tissue
Bio-compatible substrate with electrodes for recording or stimulating neuronal signals
Neuronal signals require analog-to-digital conversion, aggregation, and conversion to data packets or to human/machine-readable formats  require electronics occupying significant volume & adding significant weight to brain implant
Need lightweight, compact electronics package for BCIs

## Slide 3: Outline
Goal: Describe a method for manufacturing a sealed electrical device with “bare die” IC chip embedded within pocket of substrate & fabricated interface with direct electrical connections to IC chip
Purpose: To decrease the volume for better integration of the implant system in brain & ensuring IC chip and interface are hermetically sealed & interconnected
Embodiments:
  Vertical cross-section of sealed electrical device with embedded IC chip
  Vertical cross-section of sealed electrical device with embedded IC chip + housing
  Flowchart for manufacturing a sealed electrical device
  Flowchart for chip-first process for manufacturing a sealed electrical device
  Flowchart for chip-last process for manufacturing a sealed electrical device

## Slide 4: Vertical cross-section of sealed electrical device with embedded IC chip
Substrate
(single-crystal substrate of silicon or gallium nitride)
Pocket
(substrate with material removed)
Bare Die IC Chip
(embedded in pocket of substrate)
Connection pads
(facing outward – away from pocket)
Vias
Filler
(fill gaps between IC chip and pocket)
Polymer sheet
Hermetic coating
Hermetically seal electrical device
Applied to substrate before IC chip placed into pocket
Deposited over IC chip (to seal IC chip), conductive traces
Exposed at the site of implanted electrodes
e.g., silicon carbide, silicon oxide, hafnium oxide, diamond
Conductive traces
Patterned onto polymer sheet
Include conductive polymers (PEDOT), conductive ceramics (doped diamonds), conductive metals (gold, platinum), conductive metal-oxides (iridium oxide)
Casing
Electrodes
Ribbon cable
(formed from polymer-coated conductive traces)
- Sealed via hermetic coating
- Greater # of IC chips + conductive traces incorporated within implant
- Sealed electrical device – 30x density of typical IC chip

## Slide 5: Vertical cross-section of sealed electrical device with embedded IC chip + housing
Housing
(mounted on metal ring; enclose + seal IC chip; may be cap or lid)
Metal ring
(formed around perimeter of pocket)
Circuit board
Power input pin
Connect to components in housing to power sealed electrical device
Connect to circuit board
Include VCC (voltage > ground)
Metal ring
IC Chip
Unsealed connection pad
(e.g., power input pin)
Substrate

## Slide 6: Flowchart for manufacturing a sealed electrical device

## Slide 7: Step 1:
Substrate
(silicon wafer, glass wafer, polymer panel, or ceramic plate)

## Slide 8: Step 2:
Pocket
(etched or milled to accommodate IC chip)
Hermetic coating
(e.g., atomic layer decomposition of hafnium oxide, or chemical vapor decomposition of diamond)

## Slide 9: Step 3:
Bond pads
IC chip

## Slide 10: Step 4:
Filler
(polymer)

## Slide 11: Step 5:
Flat polymer sheet

## Slide 12: Step 6:
Conductive traces
Hermetic coating

## Slide 13: Step 7:
Electrode
Ribbon cable
(patterned polymer)

## Slide 14: Step 8:
Metal Ring
Housing
Circuit board
Substrate removed under ribbon cable
Power input pin

## Slide 15: Flowchart for chip-first process for manufacturing a sealed electrical device

## Slide 16: Step 1:

## Slide 17: Step 2:

## Slide 18: Step 3:

## Slide 19: Step 4:

## Slide 20: Step 5:
Planarized/polished filler

## Slide 21: Step 6:
Etched vias

## Slide 22: Step 7:
Bottom insulation layer

## Slide 23: Step 8:
Trace metal

## Slide 24: Step 9:
Hermetic Coating

## Slide 25: Step 10:
Vias (via etched hermetic coating)

## Slide 26: Step 11:
Top insulation layer

## Slide 27: Step 12:
Vias etched into insulation layer

## Slide 28: Step 13:
Electrode metal

## Slide 29: Step 14:

## Slide 30: Flowchart for chip-last process for manufacturing a sealed electrical device

## Slide 31: Step 1:
Etch stop

## Slide 32: Step 2:
Bottom insulation layer

## Slide 33: Step 3:
Hermetic Coating

## Slide 34: Step 4:
Conductive trace

## Slide 35: Step 5:
Hermetic Coating

## Slide 36: Step 6:
Top insulation layer

## Slide 37: Step 7:

## Slide 38: Step 8:

## Slide 39: Step 9:
Hermetic coating

## Slide 40: Step 10:
IC Chip

## Slide 41: Step 11:
Filler

## Slide 42: Step 12:
Filler planarized/polished

## Slide 43: Step 13:
Excess fill removed

## Slide 44: Step 14:
Filler etched in connection pads

## Slide 45: Step 15:
Conductive trace

## Slide 46: Step 16:
Hermetic coating

## Slide 47: Step 17:
Etch stop
Etch stop

## Slide 48: Step 18:
Hermetic coating etched
Hermetic coating etched

## Slide 49: Step 19:
Electrode metal

## Slide 50: Step 20: