## Slide 1: Glass Welding Through Non-Flat Surface
Neuralink, US 2023/0069855 A1, Published 3/9/2023
6/8/2024

## Slide 2: Background: Advantages & Drawbacks of Laser Welding
Laser welding advantages:
Greater precision compared to traditional welding techniques
  Energy applied to narrower area by laser beam, less risk of heat distortion
Enables joining of dissimilar materials, allowing welding of complex joints with ease
Laser welding drawbacks:
Laser welding becomes difficult on curved surfaces (steeper curves --> greater distortion, differing angles of incidence in laser beam)
Edge-to-edge welding presents “clipping” issues – loss of energy as laser beam approaches edge (even worse for curved surfaces)
Superficial flaws (rough finishes/residuals) absorbs energy, rending welding ineffective
Biological implants – require hermetically sealed glass housing to prevent bio-reactivity and/or bodily fluids from corroding/degrading componentry inside housing

## Slide 3: Outline
Goal: Describe method & system for laser beam welding an object with non-flat (e.g., curved) surfaces, with at least one transparent piece of the object
Purpose: Hermetically seal two pieces of hardware (with non-flat surfaces) to prevent corrosion of parts via laser beam welding
Embodiments:
  Workpiece + Optical Guide (curved surface)
  Workpiece + Optical Guide (varied surface)
  1 Workpiece embodiment
  Top + Bottom view of Optical Guide
  Cross-section view of Workpiece with Curved Surface joined by Laser Welding, utilizing clear optical guide
  Cross-section view of Workpiece Workpiece joined at an edge, utilizing an optical guide
  Flowchart of Laser Welding through Curved Transparent material

## Slide 4: Basics: Refraction (Snell’s Law)
Snell’s Law:
Index of refraction: how fast light beam travels through medium (e.g., air) vs another medium (e.g., glass)
Where – speed of light in one vacuum, – speed of light in another vacuum

## Slide 5: Workpiece + Optical Guide (curved surface)
Workpiece
Liquid optical medium
Assembly submerged in liquid optical medium
Thin layer to mitigate unwanted effects of rough finish
Fill gaps between different pieces
refractive index within 10% of index of refraction of transparent first piece
E.g., mineral oil (refractive index 1.47), lanolin, cedar wood oil, castor oil, glycerol, kerosene, etc.
Optical guide
Transparent First piece
index of refraction = 1.51
Borosilicate glass
Curved surface
First target surface
Second piece
Second target surface
Flat surface
Interface surface
* Can include ANY number of pieces

## Slide 6: Workpiece + Optical Guide (varied surface)
Varied surface
* Can include ANY number of pieces
Workpiece
Liquid optical medium
Optical guide
Transparent First piece
First target surface
Second piece
Second target surface
Flat surface
Interface surface

## Slide 7: Workpiece
Transparent First piece
permits light propagation
glass, sapphire, etc.
Made from borosilicate glass, non-silicate glass, quartz, etc.
Second piece - Same as first piece
- Can be made from same material as first piece, or metals (stainless steel, carbon steels, etc.)
Curved surface
Formed by initial fabrication of transparent first piece (e.g., molding), or via grinding process – leaving rough surfaces
Rough surface – does not allow transmission of light (can be mitigated by liquid optical medium)
First target surface
Width less than radius of first transparent piece and/or second piece – hollow space within workpiece
Second target surface
- similar to first target surface
Workpiece:
Transparent first piece + second piece
Hermetically sealed (first & second target surfaces matched together)
May contain thin-film electrodes, system-on-a-chip packages, IC packages, etc.
May be a biological implant housing, optical device (with diffractive gratings, prisms, etc.), housing for MEMS devices, sensors, etc.

## Slide 8: Top + Bottom view of Optical Guide
Top
Bottom
Width > workpiece width
(laser welding achieved regardless of workpiece width)
Depth
Optical guide extends beyond welding location (enable edge-to-edge welding)
Flat surface
depth
width
Interface surface
Concave
Form-fit curved surface
Can have ANY geometry
Optical guide
Facilitate formation of workpiece via laser welding
Made from sapphire, glass, or any transparent materia
Within 10% of index of refraction of workpiece

## Slide 9: Cross-section view of Workpiece with Curved Surface joined by Laser Welding, utilizing a Clear Optical Guide
Curved workpiece
Optical guide
Depth
width
Transparent first piece
Laser beam
(pulse freq:
1-500 * 10^-15 s)
Flat surface
Second piece
Curved surface
First target surface
Second target surface
Interface surface
Liquid optical medium
Equal or within 20% of index of refraction of transparent first piece
Mineral oil
Fill gaps between interface & curved surface
First location
Second location
Welding location
Identify first location on one piece
Identify second location on opposite piece
Define path between first and second location
Direct laser beam along path to create welds
Direct laser beam to another location to create welds
Repeat until curved workpiece is sealed (meeting / exceeding parameter)
Normal welding conditions – depth of optical guide not as deep
Laser beam
glass
refraction

## Slide 10: Cross-section view of Workpiece with Curved Surface joined at an edge, utilizing an Optical Guide
width
Laser beam
Transparent first piece
Optical guide
Flat surface
Second target surface
First target surface
Liquid optical medium
Depth
Allows edge-to-edge welding:
Extend past first target surface + covering location to be welded + partially cover second target surface
Curved surface
Second location
First location
Welding location
Curved workpiece
Second piece
Interface surface
Edge-to-edge welding – much deeper depth of optical guide (covers first target surface + welding location + second location to weld)

## Slide 11: Flowchart of Laser Welding through Curved Transparent Material

## Slide 12: Step 1:
Transparent first piece
Curved surface
First target surface

## Slide 13: Step 2:
First target surface
Curved surface
Transparent first piece
Second piece
Second target surface
Workpiece

## Slide 14: Step 3:
Curved surface
Liquid Optical Medium

## Slide 15: Step 4:
Liquid Optical Medium
Optical guide

## Slide 16: Step 5:
Laser beam
Transparent first piece
Second target surface
First target surface
Second piece
Optical guide
Flat surface
Liquid optical medium
Curved surface

## Slide 17: Step 6:
Laser beam
Transparent first piece
Second target surface
First target surface
Second piece
Interface surface

## Slide 18: Additional Steps
Identify first location on one piece
Identify second location on opposite piece
Define path between first and second location
Direct laser beam along path to create welds
Direct laser beam to another location to create welds
Repeat until curved workpiece is sealed (meeting / exceeding parameter)
Laser beam
Transparent first piece
Optical guide
Flat surface
Second target surface
First target surface
Liquid optical medium
Curved surface
Second location
First location
Welding location
Curved workpiece
Second piece
Interface surface